Make the following Section a part of the Standard Specification:

"SECTION 306 - UNTREATED PERMEABLE BASE COURSE

306.01	Description.     This work includes furnishing and placing one or more courses of untreated permeable base on a prepared surface according to the contract.

306.02	Materials.     Materials shall conform to the following:

Prime Coat for Untreated Permeable Base Course	420.02

Coarse Aggregate					703.04(A)

Filler							703.04(B)

Water							712.01

306.03	Construction Requirements.

(A)	Shoulder Preparation.     Water, shape, and compact the adjacent shoulder for a width not less than five feet and to the proposed grade for the upper surface of the permeable base course.

Provide a form or choker to retain the untreated permeable base material,  by cutting the edge of the shoulder as nearly vertical as possible with the toe of the cut located at the exterior bottom limit of the untreated permeable base material.

Dispose of the cut away material as specified by the Engineer.

(B)	Placing.     Place the coarse aggregate only upon an accepted surface.   Do not lay aggregate until the surface is dry and fully capable of supporting loaded trucks or other equipment.

Spread the coarse aggregate on the prepared surface to such a depth that when thoroughly compacted, the coarse aggregate shall be of the form and dimensions shown on the typical cross-section.

When the required thickness is nine inches or less, place the permeable base course on one layer.

When the required thickness is more than nine inches, place the permeable base course in two or more layers of approximately equal thickness.     Each layer shall have a compacted thickness of not more than nine inches.

Dump the coarse aggregate in piles upon the surface and spread by bulldozing ahead from the previously spread coarse aggregate.          When the prepared surface on which the permeable base is to be placed is stable and without a permeable separator,  the Engineer may allow the Contractor to spread the coarse aggregate When spreading,  the coarse aggregate shall be free from segregation.     Remix any segregated materials to conform to the contract.

(C)	Compacting.     Immediately after spreading a layer of coarse aggregate, use power rollers to compact the material thoroughly according to the contract.     Roll the coarse aggregate to smooth out bumps or irregularities.     The finished surface shall be within 0.04-foot of the required grade and cross-section.

Rolling shall be longitudinal to the roadway lanes.  Start at the lower edge and progress toward the higher portion of the roadbed with an overlap of at least ½  of the wheel tracks on successive trips.     Do not roll the center of the base material first.     Proceed without interruption across the area to be compacted until a minimum of eight complete coverage with the roller is attained on each lift.

After rolling the final lift of coarse aggregare, spread the filler in thin layers.     The filler shall be sufficiently dry to choke the surface voids without caking or bridging.     The layer of filler shall not exceed 30 pounds per square yard.     Roll the filler with two complete coverage.     Scatter the excess filler by light brooming.     Apply the prime coat according to Section 420 - Prime Coat for Untreated Permeable Base Course soon thereafter.     Keep all traffic,  except construction equipment directly connected with the prime coat operation,  off the permeable base.

(D)	General.     When disturbing or displacing the finished permeable base or when foreign matter enters into the base materials during storage, hauling,  or placing operations,  repair or replace such permeable materials with acceptable materials at no cost to the State.

When constructing untreated permeable base in more than one layer, construct each layer as specified above except apply the filler and the prime coat only on the top of the final layer.

The completed base shall have a firm, even surface free from bumps and irregularities.     Provide sufficient filler,  water,  brooming,  and rolling to thoroughly consolidate and compact the edges of the permeable base course to an unyielding condition.

(E)	Equipment.     Use static steel power rollers weighing not less than 10 tons.

Broom with long bristle brooms.     Standard rattan street brooms may be used when acceptable by the Engineer.

306.04	Method of Measurement.     The Engineer will measure the permeable Permeable base course will be paid on a lump sum basis.per cubic yard complete in place according to the dimensions shown on the plans or specified by the Engineer.     Measurement for pay will not apply.

306.05	Basis of Payment.     The Engineer will pay for the accepted untreated permeable base course on a at the contract lump sum basis.unit price per cubic yard.     Payment will be full compensation for the work prescribed in this section and the contract documents.

The price includes full compensation for preparing the surface;  furnishing,  applying,  and protecting the prime coat  spreading the material; furnishing,  depositing,  and placing the coarse aggregate;  disposing the excess material;  rolling;  compacting;  water for compaction;  filler for the permeable base; brooming;  and furnishing labor,  materials,  tools,  equipment,  and incidentals necessary to complete the work.

The Engineer will pay for the following pay item when included in the proposal schedule:make payment under:

Pay Item	Pay Unit

Untreated Permeable Base Course	Cubic YardLump Sum"

END OF SECTION 306