SECTION 403 - OPEN-GRADED PLANT MIX SEAL

Make the following amendments to said Section:

(I)	Amend 403.02	Materials by revising the Bituminous Material to read as follows:

"Bituminous Material (Asphalt Cement Grade AR 80)	702.01"

(II)	Amend 403.04	Method of Measurement to read as follows:by adding the following:

Method of Measurement.

(A)	Open-graded plant mix seal will be paid on a lump sum basis.     Measurement for payment will not apply.

(B)	The Engineer will measure surface preparation on a force account basis in accordance with Subsection 109.04 – Force Account Provisions and Compensation.

"The Engineer will not measure for furnishing and applying bituminous tack coat."

(III)	Amend 403.05	Basis of Payment to read as follows:

"403.05	Basis of Payment.     The Engineer will pa for the accepted pay items listed below at the contract price per pay unit,  as shown in the proposal schedule.     Payment will be full compensation for the work prescribed in this section and the contract documents.The Engineer will pay for the accepted open- graded plant mix seal at the contract price per ton complete in place.     The price includes full compensation for preparing the bituminous material and aggregates; establishing the job-mix formula; mixing and controlling the bituminous material and aggregates; transporting,  spreading,  finishing,  compacting the mixture;  furnishing and placing bituminous tack coat;  cleaning up;  sampling and testing the pavement;  and furnishing labors,  material,  equipment,  and incidentals necessary to complete the work.

The Engineer will pay for each of the following pay items when included in the proposal, schedule:

The Engineer will pay for bringing the surface to uniform grade and cross section by using Asphalt Concrete Mix No. V and applying tack coat to portland cement concrete surfaces and existing pavements on a force account basis.     The Engineer will compute for the actual amount paid according to Subsection 109.04 - Extra and Force Account Work, whether this amount is more or less than the estimated amount in the proposal.

The Engineer will make payment under:

Pay Item	Pay Unit

Open-Graded Plant Mix Seal	Ton Lump Sum

Surface Preparation	Force Account “

An estimated force account amount for preparing the surface (bringing the surface to uniform grade and cross section by using Asphalt Concrete Mix No. V and applying tack coat to portland cement concrete surfaces and existing pavements) may be allocated in the proposal schedule under ‘Surface Preparation’,  but the actual amount to be paid will be the sum shown on the accepted force account records,  whether this sum be more or less than the estimated amount allocated in the proposal.

END OF SECTION 403