Make the following Section a part of the Standard Specifications:

"SECTION 420 - PRIME COAT FOR UNTREATED PERMEABLE BASE COURSE

420.01	Description.     This work includes treating the surface of a prepared untreated permeable base course with prime coat according to the contract.

420.02	Materials.     Materials shall conform to the following:

Emulsified Asphalt (Type CSS-1h or SS-1h)		702.04

Water								712.01

420.03	Construction Requirements.

(A)	Weather Limitations.     Do not apply the prime coat when the temperature is below 60 degrees F. or on wet surfaces.     Also, do not apply the prime coat when weather conditions prevents the proper construction.

(B)	Equipment.     Provide equipment for heating and applying the prime coat.     This equipment shall conform to Subsection 405.03(B) - Equipment.

(C)	Priming.     Prime the surface immediately after the surface has been accepted by the Engineer.     The preservation of the prepared surface is the Contractor's responsibility.     Preserver, reprocess, or reshape the surface as required at no cost to the State.

(D)	Application of Prime Coat.     Dilute the emulsified asphalt (Type CSS-1h or SS-1h) with water at the rate of one part emulsion to one part of water by volume.     Submit to the Engineer the quantity, rate of application, temperature,  and areas to be treated for acceptance before applying the prime coat.     Apply the prime coat with a pressure distributor in a uniform, continuous spread.

After applying, allow the prime coat to cure before paving.     The time interval between the placement of the prime coat and the subsequent paving shall be 16 hours or more.

Apply prime coat at the rate of 0.30 to 0.40 gallon per square yard.

(E)	Protection of Prime Coat.     Keep all traffic except construction equipment directly connected with the paving operations off the prime coat. Protect the prime coat from damage until placement of the subsequent placement of the subsequent bituminous or concrete layer.

420.04	Method of Measurement.     The Engineer will not measure prime coat for payment.

420.05	Basis of Payment.     The Engineer will not pay for the prime coat separately and .     The Engineer will consider the cost for prime coat as included in the contract price of Section 306 - Untreated Permeable Base Course.     The cost is for the work prescribed in this section and the contract documents.”

The cost is for preparing the surface; and furnishing, applying, and protecting the prime coat; and furnishing labor,  materials,  equipment,  tools,  and incidentals necessary to complete the work.”

END OF SECTION 420