Amend Section 605 – Underdrains to read as follows:

“SECTION 605 - UNDERDRAINS

605.01	Description.     This section is for constructing underdrains according to the contract.

605.02	Materials.

(A)		Geotextile.     Geotextiles shall conform to Subsection 716.03 - Geotextiles for Underdrain.

(B)		Crushed Rock.     Crushed rock shall conform to Subsection 703.04 - Aggregate for Permeable Base, and to the gradation requirements of Subsection 704703.04(A) - Course Aggregate or AASHTO M 43 (ASTM D 448) size Nos. 4, No. 5, or No. 57.

(C)		Perforated Plastic Pipe.     The perforated corrugated polyethylene pipe shall conform to AASHTO M 252 or AASHTO M 294.

The perforated corrugated polyethylene pipe shall be either Type CP corrugated surface both inside and outside or Type SP corrugated wall outside and smooth inner liner.

The perforated PVC pipe shall conform to ASTM D 2729.

Submit a Certificate of Compliance to the Engineer before using the plastic pipes.

(D)		Non-Perforated Pipe. 	     Non-perforated drainpipe shall conform to the requirements of perforated pipes except that the provisions for perforation shall not apply.

(E)		Concrete.     Concrete for cleanouts shall be Class B and shall conform to Section 601 - Structural Concrete.

(F)		Steel Plate.     Steel plate for cleanouts shall conform to AASHTO M 183/M183M (ASTM A 36/A 36M).

605.03	Construction Requirements.     Excavate trenches to the dimensions and grade shown in the contract or as specified by the Engineer.

Protect the geotextiles from sunlight and temperatures over 140 degrees  F during transport and storage.     The information on the packaging shall warn against exposing the geotextile to sunlight.

Place the geotextile in the trench to conform loosely to the shape of the trench.     Overlap successive sheets a minimum of 18  inches.

Place the crushed rock in horizontal layers not exceeding 12 inches in thickness before compaction.     Compact each lift with at least two passes of a vibrating pad or drum type compactor.     Fold the geotextile over the top of the filter rock to produce a minimum overlap of 12 inches after compaction of the filter  rock.     Do not leave geotextile exposed more than five days without being covered by backfill.

Remove and replace geotextile that becomes torn or damaged observing the 18 inches overlap requirement in all directions.

Place perforated pipe with the perforations down.     Join the pipe sections securely with the appropriate couplings or bands.

Install non-perforated drain pipe of the type and size specified according to the contract or as specified by the Engineer.

605.04	Method of Measurement.     Underdrains and cleanouts will be paid on a lump sum basis.     Measurement for payment will not apply.

605.05	Basis of Payment.     The Engineer will pay for the accepted underdrains and cleanouts on a contract lump sum basis.     Payment will be full compensation for the work prescribed in this section and the contract documents.

The Engineer will pay for the following pay items when included in the proposal schedule:

Pay Item	Pay Unit

_____ Inch Underdrain Pipe	Lump Sum

Cleanout	Lump Sum”

END OF SECTION 605