Amend Section 650 - Wheelchair Ramps to read as follows:

“SECTION 650 - CURB RAMPS

650.01	Description.     This section describes constructing curb ramps at existing or new sidewalk locations.

650.02	Materials.

Concrete,  Class B

Bed Course Material for Sidewalks and Curbing	703.16(A)

Welded Wire Fabric Reinforcement	709.01(C)

650.03	Construction Requirements.     Sawcut and remove existing curb,  gutter,  and sidewalk in accordance with Subsection 202.03(D) – Removal of Concrete.

Construct curb ramps in accordance with Subsection 608.03(A) - Concrete Sidewalk and below     Reinforce with 6 x 6 – W1.4 x W1.4 welded wire fabric,  unless otherwise indicated in the contract documents.     Provide construction joints where curb ramps join existing or new sidewalks,  and where curb ramp apron abut drop curbs or gutters.

Construct drop curbs in accordance with Section 609 - Curb and/or Gutter.     Match face of drop curbs to face of abutting curbs.

Detectable warnings shall be 24 inches in the direction of travel and extend the full width of the curb ramp or flush surface.     Truncated domes shall have a diameter of 0.9 inch at the bottom,  a diameter of 0.4 inch at the top,  a height of 0.2 inch and a center to center spacing of 2.35 inches measured along one side of a square arrangement.     Domes shall be aligned on a square grid in the predominant direction of travel to permit wheels to roll between the domes.     There shall be a minimum of 70 percent contract in light reflectance between the detectable warning and an adjoining surface,  or the detectable warning shall be ‘safety yellow’.     The material used to provide visual contrast shall be an integral part of the detectable warning surface.     The detectable warning shall be located so that the edge nearest the curb line or other potential hazard is 6 to 8 inches from the curb line or other potential hazard.

650.04	Method of Measurement.     Curb ramps will be paid on a lump sum basis.     Measurement for payment will not apply.

650.05	Basis of Payment.     The Engineer will pay for the accepted curb ramps on a contract lump sum basis.     Payment will be full compensation for the work prescribed in this section and the contract documents.

The Engineer will pay for the following pay item when included in the proposal schedule:

Pay Item	Pay Unit

Curb Ramps,  Type _____	Lump Sum”

# END OF SECTION 650