Make the following section a part of the Standard Specifications:

"SECTION 655 - DRILLING HOLES AND INSTALLING

DOWEL REINFORCING BARS

655.01	Description.   This section is for drilling holes and furnishing and installing dowel reinforcing bars at abutments according to the contract.

655.02	Materials.    Materials shall conform to the following:

(A)	Reinforcing Bar.     Reinforcing bar shall conform to Section 602 - Reinforcing Steel.

(B)	Epoxy Grout.     Epoxy grout shall conform to Subsection 712.04(B) - Epoxy Grout.

(C)	Epoxy Bonding Agent.     Epoxy bonding agent shall conform to Subsection 712.02 - Epoxy Resin System.

Submit test certificates,  indicating conformance of all materials to the standards referenced herein.

655.03	Construction Requirements.

(A)	Drilling and Installation.     Do not use a heavy duty impacting drill for drilling operation.     Install dowel reinforcing bar into its place after completing the drilling to the depth shown on the plans and thoroughly cleaning the hole of all dust and residue.     Fill the hole with epoxy grout after removing all fine particles.

(B)	Traffic Control.     Traffic control shall be according to Section 645 - Traffic Control Devices,  or as specified by the Engineer.

(C)	Inspection.     Before filling the hole with epoxy grout,  inform the Engineer to inspect the hole.

655.04	Method of Measurement.     Drilled hole and dowel reinforcing bar will be paid on a lump sum basis.     Measurement for payment will not apply.

655.05	Basis of Payment.     The Engineer will pay for the accepted drilling holes and installing dowel reinforcing bars on a contract lump sum basis.    Payment will be full compensation for the work prescribed in this section and the contract documents.

The Engineer will pay for the following pay item when included in the proposal schedule:

Pay Item	Pay Unit

Drilling Holes and Installing Dowel Reinforcing Bars -

___________ Bridge	Lump Sum

# END OF SECTION 655