SECTION 709 - REINFORCING STEEL, WIRE ROPE

AND PRESTRESSING STEEL

Make the following amendment to said Section:

(I)	Amend 709.03     Prestressing Steel by revising the first paragraph to read as follows:

"709.03	Prestressing Steel.     Prestressing steel shall be:

(1)		Uncoated stress-relieved wire conforming to ASTM A 421,  or

(2)		Uncoated 7 wire low-relaxation steel strand conforming to ASTM A 416 Grade 270,  or

(3)		High-tensile alloy bars conforming to the requirements below."

END OF SECTION 709