Amend Section 305 - Aggregate Subbase Course to read as follows:

“SECTION 305 - AGGREGATE SUBBASE COURSE

305.01	Description.     This work includes furnishing and placing one or more courses of aggregate subbase on a prepared surface according to the contract.

305.02	Materials.     Materials shall conform to the following:

# Aggregate for Subbase	703.17

Water	712.01

Cullet and Cullet-Aggregate Mixtures as Construction Materials	717.01

305.03	Construction Requirements.

(A)		Placing.     Do not dump the aggregate subbase material in piles on the prepared subgrade.     Place the material in uniform layers not exceeding 6 inches after compaction.  Place and spread the material without segregation.   Remix the segregated material.    When using a vibratory roller weighing 9 tons or more,  the Contractor may increase the lift thickness to 7 inches.

The Engineer will not permit the spreading of fine material over the surface of the compacted subgrade.   Incorporate the additional material, if required,  uniformly throughout the thickness of the compacted material by scarifying and blading.  The combined material shall meet quality requirements as specified herein.

(B)		Compacting.    After spreading and compacting the aggregate subbase course, check the finished subbase for conformance with the required grade and cross-section.  The finished subbase where not controlled by adjacent structures or features shall not vary more than 0.05 foot above or below the theoretical grade.

If the base course is paid on a theoretical cubic yard basis,  the Engineer may waive the lower finish surface tolerance.

Compaction of each layer shall continue until a density of not less than 95% of the maximum density according to Subsection 203(C)(2) – Relative Compaction Test is achieved.

The Engineer will make the field density determination according to Hawaii Test Methods HDOT TM 1,  2,  and 3 .  Maintain the surface of each layer during the compaction operations so that a uniform texture is produced and the aggregate is firmly keyed.

305.04	Method of Measurement.     Aggregate subbase will be paid on a lump sum basis.     Measurement for payment will not apply.

305.05	Basis of Payment.     The Engineer will pay for the accepted aggregate subbase on a contract lump sum basis.     Payment will be full compensation for the work prescribed in this section and contract documents.

The Engineer will pay for the following pay item when included in the proposal schedule.

Pay Item	Pay Unit

Aggregate Subbase	Lump Sum”

## END OF SECTION 305