Amend Section 311- Asphalt Treated Permeable Base to read as follows:

“SECTION 311 - ASPHALT TREATED PERMEABLE BASE

311.01	Description.     This section is for constructing an asphalt treated permeable base (ATPB) to the lines, grades,  and dimensions according to the contract.

311.02	Materials.     Materials shall meet the following:

Asphalt Cement (Grade AR 80)	702.01

Cullet Materials for Roadway 	717.02

The aggregate shall conform to Subsection 703.09 – Aggregate for Hot Plant Mix Bituminous Pavement- except that the grading requirement shall be:

| Sieve Designation | Percent Passing By Weight |
| --- | --- |
| 1.0 Inch | 100 |
| 0.75 Inch | 90 – 100 |
| 0.5 Inch | 35 – 65 |
| 0.375 Inch | 20 – 45 |
| No. 4 | 0 – 10 |
| No. 8 | 0 – 5 |
| No. 200 | 0 – 2 |

ATPB includes a mixture of aggregate and asphalt binder according to the contract.

Add bituminous binder in an amount between 2 percent to 3 percent based on the dry weight of the aggregate to the mixture as specified by the Engineer.

Measure the asphalt content of the asphalt mixture by the nuclear gage according to Hawaii Test Method 25.

311.03	Construction Requirements.

(A)		Preparation of Surface.     The surface shall conform to the compaction and elevation tolerances specified for that surface involved.  Also, the surface shall be free of loose or extraneous material.

When the prepared surface is untreated base, subbase,  or subgrade,  apply prime coat to prepared surface.  Prime coat shall conform to Section 408 - Prime Coat.

(B)		Storing, Proportioning, and Mixing.     Store, proportion,  and mix the materials for ATPB according to Subsection 401.04 - Bituminous Mixing Plant Requirements and Process,  401.04(A) - Plant Operation,  and 401.05(B)(1) - Hauling Equipment except:

(1)	The Contractor need not separate the aggregate into sizes.

(2)	Do not use ATPB  stored over two hours in the work.

(C)		Placing, Spreading,  Compacting, And Shaping ATPB.     Placing of ATPB shall conform to Subsections:

(1)	401.05(B)(2) - Bituminous Pavers,

(2)	401.05(B)(3) - Rollers,

(3)	the first paragraph of 401.05(D) - Spreading and Finishing, and

(4)	401.05(E) - Compaction.

Place ATPB in compacted lifts not exceeding 6 inches.    Compact each lift with one complete coverage of with a steel-tired,  two-axle tandem roller weighing not less than 8 tons nor more than 12 tons.     Compaction shall begin when the temperature of the base mixture is less than 150 OF.  Also,  complete the compaction before the base mixture is less than 100 OF.  Do not cool the ATPB with water.

The Contractor may use the vibratory rollers meeting the above requirements provided the vibratory unit is turned off.

The finished surface of ATPB shall be uniform and shall not vary more than 0.5 inch above or below the grade according to the contract.

Prevent contamination of the ATPB.     Remove and replace the contaminated ATPB at no cost to the State.

Repair damages to the ATPB promptly at no cost to the State and according to the contract.

(D)		Surfaces Not Within Tolerance.     Remove and replace the ATPB with a surface higher than 0.5 inch above the grade established by the Engineer with ATPB that complies with the contract.     When permitted by the Engineer,  the Contractor may remove high spots to within specified tolerance by methods that does not produce contaminating fines nor damage the base to remain in place.    The Engineer will not permit grinding.

Remove and replace hardened ATPB with a surface lower than 0.5 inch below grade established by the Engineer with ATPB that complies with the contract.     When permitted by the Engineer, fill the low areas with asphalt concrete conforming to the requirements for the lowest layer of asphalt concrete to be placed as pavement.     Do this as a separate operation before placing the lowest layer of pavement.

311.04	Method of Measurement.     The Engineer will measure the ATPB will be paid on a lump sum basis.per ton according to Subsection 109.01 - Measurement of Quantities except the Engineer will not require conversion of ATPB quantity to tonnage based on bulk (dry) specific gravity.     There will be no allowance for ATPB placed outside said dimensions.     Measurement for paymentwill not apply.

311.05	Basis of Payment.     The Engineer will pay for the accepted ATPB on a at the contract lump sum basis.unit price per ton.     Payment will be full compensation for the work prescribed in this section and the contract documents.

The price includes full compensation for preparing the surface;  storing, proportioning,  mixing,  and transporting the ATPB;  placing,  spreading,  compacting, and shaping the ATPB;  removing and filling low areas with ATPB or filling low areas with asphalt concrete;  and furnishing materials,  labor,  tools,  equipment,  and incidentals necessary to complete the work.

The Engineer will pay for the following pay item when included in the proposal schedule:make payment under:

Pay Item									Pay Unit

Asphalt Treated Permeable Base	TonLump Sum”

END OF SECTION 311