Amend Section 412 – Paving Fabric to read as follows:

# “SECTION 412 - PAVING FABRIC

412.01	Description.     This work includes furnishing and placing paving fabric and asphalt cement between pavement layers.

412.02	Materials.     Materials shall meet the following:

Asphalt Cement (PG 64-16)	702.01

Paving Fabric	716.04

412.03	Construction Requirements.

(A)	Weather Limitations.  Application of asphalt cement will not be allowed under the following conditions:

(1)	On wet surfaces, as determined by the Engineer.

(2)	When air temperature is below 60 degrees F and falling.     Asphalt cement may be applied when air temperature is above 50 degrees and rising.     Air temperature will be measured in shade and away from artificial heat.

(3)	When weather conditions prevent proper method of construction.

(B)	Equipment.  Provide equipment for heating and distributing asphalt cement according to Subsection 407.03(B) - Equipment.

(C)	Surface Preparation.     Immediately before applying the asphalt cement,  clean surface in accordance with Section 310 – Brooming Off.

Clean cracks and joints with compressed air.  Seal cracks and joints wider than 3/8 inch with sand slurry consisting of 20 percent CSS-1 emulsified asphalt, approximately 2 percent portland cement, water, and blending sand.

Clean potholes and other surface defects and fill with Hot Mix Asphalt Pavement, Mix V.

(D)	Application of Asphalt Cement Binder.     Protect all structures, including guardrails, guardrail post, and other appurtenances, from asphalt cement splatter.

Apply asphalt cement to cover area of paving fabric plus 3 inches on each side.

Limit asphalt cement application only to areas that can be immediately covered with paving fabric and that can be paved on same day.     Do not allow asphalt cement to chill, set up, dry, or otherwise impair placement of paving fabric.

Apply asphalt cement at rate of 0.25 gallons asphalt per square yard or as recommended by the paving fabric manufacturer.     Temperature of asphalt cement at time of spraying shall be between 290 degrees F and 325 degrees F.

(D)	Paving Fabric Placement.     Before asphalt cement has cooled and lost its tackiness, place fabric onto asphalt cement, with heat-bonded side up and with minimum wrinkling or folding.

Slit, lay flat, and tack all wrinkles or folds 1/2 inch or more in height.     Broom or roll paving fabric to remove air bubbles and maximize fabric contact with pavement surface.

Overlap fabric 6 inches at joints.  Do not lap joint with more than two layers of fabric.  Shingle transverse joints in direction of paving.  Apply asphalt cement to fabric joints at rate of 0.2 gallons per square yard, or as recommended by paving fabric manufacturer.

Construction equipment or vehicular traffic will not be allowed directly on paving fabric.

Remove and replace damaged paving fabric at no additional cost to the State.

(F)	Paving Operation.     Construct hot mix asphalt overlay indicated in the contract documents in areas where fabric has been placed during same day as fabric placement.     If asphalt cement bleeds through paving fabric prior to placement of hot mix asphalt overly,  blot asphalt cement by spreading same type of hot mix asphalt mixture on affected areas.     Limit hot mix asphalt laydown temperature to a maximum of 325 degrees F.     If paving fabric is composed of polypropoylene material,  limit laydown temperature to a maximum of 300 degrees F.

412.04	Method of Measurement.     The Engineer will measure paving fabric per square yard of fabric finished surface,  not including overlaps.

The Engineer will measure hot mix asphalt overlay under Section 401 – Asphalt Concrete Pavement

412.05	Basis of Payment.     The Engineer will pay for the accepted paving fabric at the contract unit price per square yard.Payment will be full compensation for the work prescribed in this section and the contract documents

The Engineer will pay for the following pay item when included in the proposal schedule::

## Pay Item	Pay Unit

Paving Fabric	Square Yard”

The Engineer will pay for:

(1)	20% of the contract bid price upon completion of preparing the surface;

(2)	30% of the contract bid price upon completion of furnishing and applying the asphalt cement binder;

(3)	40% of the contract bid price upon completion of furnishing and placing of the paving fabric;

(4)	10% of the contract bid price upon completion of cleaning up;

The Engineer will pay for the accepted hot mix asphalt overlay under Section 401 – Asphalt Concrete Pavement.

END OF SECTION 412