Make the following Section a part of the Standard Specifications:

"SECTION 413 - RECYCLED ASPHALT CONCRETE PAVEMENT

413.01	Description.     This work includes furnishing and placing recycled asphalt concrete pavement (Recycled ACP) according to the contract.

413.02	Materials.     The recycled ACP includes a mixture of crushed reclaimed asphaltic concrete pavement (RAP), virgin aggregate, and asphalt cement.     The Contractor shall select the exact proportion of crushed RAP to virgin aggregate in the mix.     However, the proportion of crushed RAP to virgin aggregate shall not exceed 20 percent by weight.

The Contractor shall conform to the following requirements:

Bituminous Material (Asphalt Cement, Grade AR 80)	702.01

Aggregate for Plant Mix Asphalt Concrete Base Course	703.03

Blending Sand	703.22

Process the RAP to provide a reasonably uniform gradation from fine to coarse with 100 percent of the material passing the three-quarter inch sieve.     The extracted bitumen content for the crushed RAP shall be not less than 2% when tested according to AASHTO T 164.     Handle and size the virgin aggregate material such that the blend of the crushed RAP material and the virgin aggregate material results in a reasonable and acceptable gradation.     The Engineer will establish a job tolerance for the combined mixture.     Once the job mix is established, maintain controls to produce a uniform product as established in the job mix.

Submit, for acceptance, a recycled  job-mix formula for the project.     The job-mix formula shall indicate the source of aggregate, grade of bituminous material, and the proportion of crushed RAP to be used in the mixture.     Furnish only one grade of bituminous material and one recycle proportion for the project. Make grade or proportion changes only upon written permission by the Engineer.

The established recycled ACP mixture shall have an air void content of four percent to six percent and have a minimum stability of 37 when tested according to ASTM D 1561.     The total amount of bituminous binder in the recycled ACP mixture shall be between four percent and six percent.

Do not start recycled ACP work on the project until:

(1)		submitting samples of the materials intended for use and

(2)		the Engineer accepts the asphalt content.

Submit samples no less than 15 working days before recycled ACP work.

The Engineer will permit the use of a nominal quantity of blending sand not exceeding five percent of the total weight of aggregate for the purpose of obtaining a satisfactory grading of the materials composing the mixture.

413.03	Construction Requirements.     Construction methods shall conform to Subsection 401.03, except as specified herein.

(A)		The equipment shall conform to Subsection 401.03(B), except as follows:

(1)	Requirements for All Plants.

(a)	Heat the virgin aggregate material to result in a finished mixed temperature of approximately 290 degrees F.     Control weighing and mixing operations to optimize heat transfer from virgin aggregate material to the reclaimed aggregate material.

(c)	Use an appropriate method to add the crushed RAP material to the heated virgin aggregate material.     This method shall allow the crushed RAP material to be added after the virgin aggregate material has left the drier.     The method shall provide a positive control on proportioning of the crushed RAP material into the mixture.     The Contractor shall:

1.	feed the crushed RAP material to an accuracy of 10% of the required weight;

2.	have a maximum moisture content of 1% after mixing the crushed RAP material with the heated virgin aggregate

3.	retain the recycled ACP mixture in a single silo to optimize heat transfer and promote continuous batching.

(2)	Requirements for Drier-Drum Plants.     Feed the crushed RAP material directly into the weigh hopper or pugmill.

(3)	Requirements for Drier-Drum Plants.     Design the cold-feed system to prevent direct flame impingement on the crushed RAP material being recycled.     Conform to Subsection 401.03(B)(1)(d)4 - Proportioning for Drier-Drum Mixing with Cold-Feed Control.

(4)	Paver.     Equip the paver with an electronic screed control device accepted by the Engineer.     The electronic device may include a grade controlling sensor mounted on each side of the paver.     Each sensor may take its grade reference from a 10-foot ski for the first pass.     The Contractor may substitute one ski with a joint shoe riding on the finished adjacent pavement for subsequent passes.

(B)		Criteria on Mat Thickness.     The criteria on mat thickness shall be as follows:

(1)	When the required thickness of recycled ACP is less than three inches, spread and compact the mixture in one layer.

(2)	When the required thickness of recycled ACP is three inches or more, spread and compact the mixture in two or more layers of approximately equal thickness.     The minimum compacted thickness of one layer shall be one and a half inches.

(C)		Unavailability of Recycled ACP.     When recycled ACP is not available, furnish regular ACP conforming to Section 401 - Asphalt Concrete Pavement in place of recycled ACP and at the same contract unit price. Notify the Engineer and obtain permission before such work.

(D)		Brooming Off.     Brooming off shall conform to Section 310 - Brooming Off.

(E)		Sampling.     Cut samples from the compacted pavement for testing within 24 hours of lay down.     The cut pavement samples shall be 12 inches by 12 inches or four-inch diameter cores, minimum.     Take samples of the mixture for the full depth of the course at the location as specified by the Engineer.     Place and compact new material to conform with the surrounding area after taking samples.     Consider the cost of sampling and restoring the area incidental to recycled ACP.

(F)		Tack Coat.     Apply tack coat to layers of recycled ACP for multiple lift construction.     Tack coat shall conform to Section 407 - Bituminous Tack Coat.

413.04	Method of Measurement.     The Engineer will measure recycled Recycled ACP will be paid on a lump sum basis.per ton according to Section 109 - Measurement and Payment.     The Engineer will not require conversion of a base course quantity to tonnage based on bulk (dry) specific gravity.     Measurement for payment will not apply.

413.05	Basis of Payment.     The Engineer will pay for the accepted recycled ACP on a lump sum basis.at the contract unit price per ton.     Payment will be full compensation for the work prescribed in this section and the contract documents.

The price includes full compensation for handling, salvaging, and reprocessing operations of the RAP; brooming off;  furnishing and applying bituminous tack coat;  furnishing,  spreading,  and compacting the recycled ACP; sampling;  restoring the area;  and furnishing materials,  equipment,  tools,  labor, and incidentals necessary to complete the work.

The Engineer will pay for the following pay item when included in the proposal schedule:make payment under:

Pay Item							Pay Unit

Recycled Asphalt Concrete Pavement					TonLump Sum"

END OF SECTION 413