Amend Section 608 - Sidewalks to read as follows:

“SECTION 608B – ASPHALT CONCRETE SIDEWALKS

608B.01	Description.     This section describes constructing asphalt concrete sidewalks.

608B.02	Materials.

## Asphalt Concrete Pavement Mix No. V	401

Bed Course Material for Sidewalks and Curbing	703.16(A)

Increase asphalt content for Asphalt Concrete Pavement Mix No. V at least 0.5 percent above that used for asphalt concrete pavements.

608B.03	Construction Requirements

(A)	Excavating.   Excavate to required depth and compact subgrade to firm, even surface.     Replace soft and yielding material with accepted material and compact.

(B)	Forms.     Use full-depth wood or metal forms that are straight,  free from warp and of sufficient strength to resist pressure of asphalt concrete without springing.     Brace and stake forms to remain in both horizontal and vertical alignment until removal.

(C)	Bed Course.     Use aggregate for untreated base in accordance with Subsection 703.16(A) - Bed Course Material for Sidewalks and Curbing,  as bed course material.     Place bed course material a minimum of 4 inches in depth.     Compact with at least three passes of lightweight mechanical tamper, roller, or vibratory system.

(D)	Placing Asphalt Concrete.  Place asphalt concrete on compacted base course to the required depth.  Compact asphalt concrete with hand operated or power roller.  Hand tamp areas inaccessible to roller.  Compact asphalt to 90 percent of maximum theoretical density according to AASHTO T 209.

(E)	Finishing.     Finish sidewalk as plane surface with 2 percent cross slope towards  roadway.

(F)	Backfilling.     After sidewalk has set,  fill remaining excavated areas with accepted material.  Place and tamp accepted material in layers up to 6 inches in depth.

608B.04	Method of Measurement.     Asphalt concrete sidewalk will be paid on a lump sum basis.     Measurement for payment will not apply.

608B.05	Basis of Payment.     The Engineer will pay for the accepted asphalt concrete sidewalk on a contract lump sum basis.     Payment will be full compensation for the work prescribed in this section and the contract documents.

The Engineer will pay for the following pay item when included in the proposal schedule:

Pay Item	Pay Unit

Asphalt Concrete Sidewalk	Lump Sum”

# END OF SECTION 608B