# SECTION 646 - GEOCOMPOSITE DRAIN

646.01	Description.     This section describes furnishing and placing geocomposite drains on slopes and walls not exceeding 8 feet in height.

646.02	Materials.

(A)	Geocomposite Material.     Geocomposite material shall pass water while retaining soil without clogging.     One side of the geocomposite material shall be impermeable.     The geocomposite material shall be resistant to chemical attack,  mildew and rot.     The material shall conform to the following minimum average roll value (MARV) for every test property listed below:

| PROPERTY | TEST PROCEDURE | REQUIREMENTS |
| --- | --- | --- |
| Fabric Properties: |
| Tensile Strength, either direction, (lbs) (minimum) | ASTM D 4632 | 110 |
| Elongation, either direction (%) (maximum) | ASTM D 4632 | 70 |
| Puncture Resistance (lbs) (minimum) | ASTM D 4833 | 70 |
| 1 Apparent Opening Size (US Standard Sieve) | ASTM D 4751 | 70 - 120 |
| Core Properties: |
| Compressive Strength (psi) (minimum) | ASTM D 1621 | 40 |
| Flow Rate at 14.5 psi, gradient 1.0 (gal/min/ft) (minimum) | ASTM D 4716 | 15 |
| 1 Apparent Opening Size (AOS) requirement may be adjusted by the Engineer when less than 50 % of the soil particles by weight passes US No. 200 Sieve or when permeability (ASTM D 4491) of the geotextile is equal to or less than permeability of the soil. |

The Contractor shall furnish a Certificate of Compliance with each shipment of materials attesting that the geocomposite material conforms to the contract.

(B)	Perforated Pipe.     Perforated pipe shall conform to the following:

Plastic Pipe	706.12

Corrugated Metal Pipe for Underdrains	707.04

The Contractor shall have the option of installing either type of pipe listed above.     The Contractor shall not mix the types of pipe within the ends of the installation.

(C)	Nonperforated Pipe.     Nonperforated pipe shall conform to perforated pipe except that the provisions for perforation shall not apply.

(D)	Structure Backfill.    Structure backfill material "A" shall conform to Subsection 703.20 - Structure Backfill Material.

646.03	Construction Requirements.

(A)	Packaging and Storing.     Furnish geocomposite rolls with suitable wrapping for protection against moisture and ultra-violet exposure before placement.     Identify,  store,  and handle each roll according to ASTM D 4873.     If stored outdoors,  elevate and protect them with waterproof cover.

(B)	Geocomposite Material Exposure Following Placement.     Exposure of geocomposite drain material to the elements between laydown and cover shall be a maximum of five days to minimize damage potential and  deterioration.

(C)	Site  Preparation.     Before placing geocomposite material,  clear the ground site of sharp objects,  cobbles, boulders and vegetation.     Excavate the rock protruding surfaces to neat lines.     Backfill voids and over excavations with structure backfill material "A" as required to produce neat lines.

(D)	Installation.

(1)	When placing geocomposite drain on slopes,  unroll and place the geocomposite material on the prepared surface with the permeable fabric face against the subgrade.     Do not drag the geocomposite material on the ground.

(2)	If placing geocomposite drain on walls,  provide mastic or other accepted material.     Use hand operated compaction equipment no closer than one foot away from the geocomposite drain material.

(3)	At geocomposite drain joints,  peel back the fabric from the core material and provide a minimum fabric overlap of 3 inches.     At the ends of the drainage panel,  provide a 3 inch lap over the edge of the core material.     To connect the perforated pipe,  peel back fabric from the core a sufficient distance to encircle the perforated pipe between the fabric and core materials with a minimum of 3 inch fabric lap over the core material.

(4)	Place the perforated pipe with the perforations down.     Join the pipe sections securely with appropriate couplings and/or bands.

(E)	Damage Repair.     Remove and replace torn,  punctured,  or damaged geocomposite material areas with undamaged geocomposite material at no increase in contract price or contract time.    Make repair observing the minimum overlap requirements specified above.

646.04	Method of Measurement.     Geocomposite drain and perforated drain pipe will be paid on a lump sum basis.     Measurement for payment will not apply.

646.05	Basis of Payment.     The Engineer will pay for the accepted pay items listed below at the contract price per pay unit shown below.     Payment will be full compensation for the work prescribed in this section and the contract documents.

The Engineer will pay for each of the following pay items when included in the proposal schedule:

Pay Item	Pay Unit

Geocomposite Drain	Lump Sum

___-Inch Perforated Drain Pipe	Lump Sum

The Engineer will pay for excavation and backfill in accordance with and under Section 206 - Excavation and Backfill for Drainage Facilities.

END OF SECTION 646