## SECTION 712 - MISCELLANEOUS

Make the following Subsection a part of said Section:

Amend 712.57     Hot Applied Rubberized Sealant by revising the table to read as follows:

| "TESTS | SPECIFICATIONS LIMITS |
| --- | --- |
| Brookfield Viscosity at 400 OF. (ASTM D 3236) | 75 poise maximum |
| Penetration, 125 OF., 50g. 5 seconds (ASTM D 5) | 50 maximum |
| Penetration, 77 OF., 100g. 5 seconds (ASTM D 5) | 10 - 25 |
| Softening Point (ASTM D 36) | 210 OF. |
| Ductility, 77 OF. (ASTM D 113) | 15 cm minimum |
| Flexibility, 0 OF. Crafco Procedure | Pass |
| Recommended Pour Temperature | 380 OF. |
| Safe Heating Temperature | 420 OF. |
| Specific Gravity at 60 OF. (material purity) | 1.05 maximum" |

# END OF SUBSECTION 712.57