SECTION 703 – AGGREGATES

Make the following amendments to said Section:

- Amend TABLE 703.01-3 FINE AGGREGATE GRADING REQUIREMENTS, HAWAII AND KAUAI   to read as follows:

“

| TABLE 703.01-3 - FINE AGGREGATE GRADING REQUIREMENTS, HAWAII AND KAUAI |
| --- |
| Sieve Sizes | Percent Passing by Weight |
|  | Calcareous Sand | Crusher Screenings |
| 3/8 Inch | 100 | 100 |
| No. 4 | 95 – 100 | 95 - 100 |
| No. 8 | - | 50 - 85 |
| No. 16 | - | 32 - 60 |
| No. 30 | - | - |
| No. 50 | - | 15 - 30 |
| No. 100 | 0 – 5 | 5 - 20 |

“

# END OF SECTION 703