SECTION 312 – HOT MIX GLASSPHALT BASE COURSE

Make the following amendments to said Sections:

(I)	Amend Section 312.03(C) Compaction by revising the second paragraph, from line 102 to 105, to read as follows:

“Compact mixture immediately upon completion of spreading operations to density of not less than 92.0 percent of maximum theoretical specific gravity in accordance with AASHTO T 209, modified by deletion of Supplemental Procedure for Mixtures Containing Porous Aggregate.”

(II)	Amend Section 312.04     Measurement, from line 116 to 117 to read as follows:

“312.04 	Measurement.

(A)	HMGB course will be paid on a lump sum basis.     Measurement for payment will not apply.

(B)	The Engineer will measure HMGB course per ton in accordance with contract documents.”

(III)	Amend Section 312.05     Payment, from line 119 to 139, to read as follows:

“312.05 	Payment.     The Engineer will pay for the accepted pay items listed below at the contract price per pay unit, as shown in the proposal schedule.      Payment will be full compensation for the work prescribed in this section and the contract documents.

The Engineer will pay for one of the following pay items when included in the proposal schedule:

Pay Item	Pay Unit

(A)	Hot Mix Glassphalt Base Course 	Lump Sum

(B)	Hot Mix Glassphalt Base Course	Ton

- 80% of the contract unit price upon completion of submitting a job-mix formula acceptable to the Engineer; preparing the surface, spreading, and finishing the mixture; and compacting the mixture by rolling;

- 20% of the contract unit price upon completion of cutting samples from the compacted pavement for testing; placing and compacting the sampled area with new material conforming to the surrounding area; protecting the pavement; and final analysis.

The Engineer may, in lieu of requiring removal and replacement, use the sliding scale factor to accept HMGB compacted below 92.0 percent.  The Engineer will make payment for the material in that production day at a reduced price arrived at by multiplying the contract unit price by the pay factor shown in Table 312.05-1.

| Table 312.05-1 – Sliding Scale Pay Factor |
| --- |
| Percent Compaction | Percent Payment |
| 92.0 or greater | 100 |
| 90.0 – 91.9 | 80 |
| <90.0 | Removal |

“

END OF SECTION 312

# Comments

Use lump sum if the project is quantifiable and plans are well defined. Otherwise use ton. The State or County Design Engineer has a final say also based on the nature of the work item, and the project or scope of work.