SECTION 706 - CONCRETE, CLAY AND PLASTIC PIPE

Make the following amendments to said Section:

(I)	Amend Subsection 706.02(A)  RCP for Drainage System from lines 8 to 28 to read as follows:

“(A)	RCP for Drainage System.  RCP shall conform to AASHTO Load and Resistance Factor Design (LRFD) specifications, and AASHTO M 170 for specified diameters and strength class, and requirements below:

(1)	Acceptance shall be based on:

(a)	Plant Certification from the American Concrete Pipe Association (ACPA), National Precast Concrete Association (NPCA), or Precast/Prestressed Concrete Institute (PCI).

(b)	Certified Plant Load Bearing Test results.

(c)	Certified Material Test results.

(d)	Inspection for visual defects and imperfections of the manufactured pipe.

(2)	Using three-edge-bearing test method, pipe shall be loaded until 0.01-inch crack occurs.  Pipe manufacturer shall furnish facilities and provide personnel to perform test according to AASHTO T 280 (ASTM C 497). Each section of pipe, in addition to required pipe markings, shall include project identification and inspection lot designation.

(3)	Precast reinforced concrete pipe end sections shall conform to the requirements above.”

# END OF SECTION 706